## Slide 1
Comparison of CPTA and Hamamatsu SiPMs
M.Danilov
ITEP
2nd open meeting of
Super KEKB Collaboration
19/03/2009 KEK

## Slide 2
We consider two types of SiPMs as photodetectors for the scintillator KLM
CPTA MRS APD
796 40um pixels, 1.28 mm inscribed circle
Hamamatsu MPPC
667 50um pixels, 1.3x1.3 mm^2
556 pixel version of CPTA SiPM

## Slide 3
MGPD PROPERTIES

## Slide 4
PDE spectral dependence at maximum bias voltage
(Yu.Musienko)

## Slide 7
Irradiation leads to similar dark current increase in MPPC and MRSAPD
Individual p.e. peak are smeared after ~10^10 p/cm^2
However MPPC show fast annealing after irradiation with neutrons

## Slide 8
Annealing of MRSAPD is slower than of MPPC?
More studies required

## Slide 9
Summary
MRSAPD and MPPC are practically identical in size and in number of pixels
MRSAPD has slightly higher PDE
MRSAPD has somewhat smaller X-talk and after-pulses
MPPC has shorter pulses and no signal tail
MPPC has 4 times smaller dark counting rate
MPPC has better uniformity of parameters but PDE varies a lot for fixed gain
MRSAPD has ~8 times smaller sensitivity to temperature variations
MRSAPD has ~3 times smaller sensitivity to voltage variations
MRSAPD is slightly cheaper (subject to negotiations)
MPPC will have high statistics data on long term stability soon (from T2K)
(SiPMs from MEPhI demonstrated excellent long term stability in
ILC calorimeter prototype- only 5 dead photo-detectors out of 8000 in 3 years)
MRSAPD and MPPC show similar increase of dark current after irradiation
but MPPC has faster annealing (to be checked)
Both photo-detectors are adequate for the SuperKEKB KLM
However there is very little safety margin in radiation hardness