## Slide 1: Light Output measurement of BSO scintillator
2009/July/7th
Tomoko Iwashita/Kenkichi Miyabayashi

## Slide 2: Outline
Motivation
  BSO is an alternative option;
  Heavier and longer wavelength(~480nm).
  Checked Light Output of small samples quickly.
Set up
ADC distribution
  PureCsI
  BSO
Compared with PureCsI
Summary and plans

## Slide 3: Set up
・PMT : H3167(19mmφ)
Borosilicate glass window
Bialkali photocathode
HV → 1650V
Scintillator
PMT
Radiation source 137Cs(662keV)
AMP
Div
AMP
ATT
Discri
G.G.
Charge-sensitive ADC(LeCroy2249W)
Width 500ns
Veto 1ms
Optical grease
Threshold
20mV～30mV
To match ADC range

## Slide 4: Samples
PureCsI
1φ×2cm
BSO
1*1*2cm3 BSO both ends mirror polish, 4 side surfaces are frosted.
Wrapped by white Gore-TeX film.

## Slide 5: ADC distributionof PureCsI
Size : 1φ×2cm. (λ=330nm)
Around photoelectric peak is magnified as right figure, together with fitted line by Gaussian.
Photoelectric peak
Compton scattering

## Slide 6: ADC distribution of BSO
Size : 1cm×1cm×2cm.
(Purity 99.9999%, λ=480nm)
ATT 6dB : To adjust ADC range.
Right figure is magnification around photoelectric peak.
Compton scattering
Photoelectric peak

## Slide 7: To compare with PureCsI
L.O. of BSO is two times as PureCsI.
Sample
L.O. (PureCsI equal 1 )
BSO SA, SB and No.1 are different samples; all purity 99.9999%.
Chart: 
| LuAG | LuAG(Sylinder) | BSOSA | BSOSB | BSONo1
 | 5.553 | 6.811 | 1.884 | 1.496 | 1.953
.
As for Pr:LuAG,
see 2008 Dec. meeting slides
BSO exhibits double effective L.O. because of longer wavelength!

## Slide 8: Comments on sample dimension and surface finishing.
Light collections for PureCsI(cylindrical)=BSO(1X1X2cm3) assumed.
In order to make sure, PureCsI (1X1X2cm3) ordered, delivered in 3 weeks.
Then answer becomes clearer.

## Slide 9: Actually we experienced;
L.O. of 2x2x2cm3 BSO(all 6 surfaces mirror polished) exhibits ~ half of 1x1x2cm3(only both end surfaces are mirror polished) sample.
  Though they are taken from the exactly same block.
Thought to because of photon’s total reflection at its polished surfaces ~45 deg.
Significant amount of photons are absorbed during travel inside crystal…
x
Common phenomena in crystal with n>sqrt(2).
Notes: 9

## Slide 10: Summary and plans
Effective L.O. of BSO is 2 times as high as PureCsI because of longer wavelength.
1*1*2cm3 PureCsI (Both ends mirror polish, 4 side surfaces are frosted) will be gotten soon.
  To remove possible light collection difference .
Radiation hardness test of BSO(and Pr:LuAG) small samples.

## Slide 11: Back up

## Slide 12: Typical Photocathode Spectral Response and Emission Spectrum of Scintillators
PureCsI
BSO
From HAMAMATSU text